Ligends for Figs.

Fig. 1		Chemical analysis of representative sample of stibnite.

Fig. 2		Colonies of bacterial strain on semisolid medium

Fig. 3 		Microscopic view of isolated Thiobacillus ferrooxidans

Fig. 4  		Initial to final stage of medium having Bacterial strain

Fig. 5 		Direct application of microbial strain on roll crushed ore sample of antimony

Fig. 6		Effect of the pH on bioleaching of antimony from stibnite

Fig. 7		Effect of time period on bioleaching of antimony

Fig. 8		Effect of temperature on the bioleaching of antimony

Fig. 9		Effect of grain size on bioleaching of antimony

Fig. 10		Effect of aeration speed on bioleaching of antimony

Fig. 11		Flow diagram for the process of antimony ore

Fig. 12	 	Final product antimony sulphide

Legends for Tables

Table 1		Recovery of antimony on optimal conditions

Fig. 1	Chemical analysis of representative sample of stibnite.

Fig. 2	Colonies of bacterial strain on semisolid medium

Fig. 3 	Microscopic view of isolated Thiobacillus ferrooxidans

Fig. 4  		Initial to final stage of broth culture of bacterial strain

Fig.5 	Direct application of microbial strain on roll crushed ore of antimony

FLOW SHEET FOR BIOLEACHING OF ANTIMONY

Antimony Ore

Crushing & Grinding

Over size

Sieving

Bacterial Leaching

Solvent Extraction

Extraction of antimony as antimony Sulphide

Fig. 11	Process flow diagram for bioleaching of antimony

Fig 12	Final product antimony sulphide

Table 1 		Recovery of antimony on optimal conditions

| Weight of the ore | Volume of Bacterial Strain | Grain size | Shaking speed | Temperature (°C) | Time period (Days) | Recovery of metal |
| --- | --- | --- | --- | --- | --- | --- |
| 100 grams | 1000ml | -150# | 100 rpm | 37°C | 120 days | 73% |