Table and Figures Captions

**Table1:** ICP operating conditions

Table2: Effect of TOA% on palladium extraction in different solvents.

Table3: Effect of different stripped agents

Figure1: Effect of TOA% on palladium extraction in different solvents (a: toluene, b: xylene, c: crosin and d: 1, 2 dichloroethane).

**Figure2:** Variation of the palladium (Ⅱ) extraction with the HCl concentration (200 ppm Pd (Ⅱ) in 0.05-8 M; 2.5% TOA in toluen; A: O (v/v) = 1; room temperature; 10 min).

**Figure3:** The effect of HClO4 concentration on stripping

Figure4: The effect of H2SO4 concentration on stripping

**Figure5:** The effect of NH3 concentration on stripping

Table 1: ICP operating conditions

|  |  |
| --- | --- |
| Plasma view | axial |
| Analysis time | 0.5 s |
| Plasma gas flow rate | 150 L / min |
| Sample flow rate | 1.5 mL / min |

Table 2: Effect of TOA% on palladium extraction in different solvents.

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| TOA% | T ( min ) | toluene % | xylene % | crosin % | 1, 2 dichloroethane % |
| 12.5510 | 5 | 99.99799.99899.99899.998 | 99.99699.99899.99899.998 | 99.99599.99699.99699.994 | 99.99799.99899.99899.998 |
| 12.5510 | 10 | 99.99899.99999.99899.998 | 99.99799.99899.99899.998 | 99.99599.99699.99699.994 | 99.99899.99899.99899.998 |
| 12.5510 | 15 | 99.99999.99999.99899.998 | 99.99799.99899.99899.998 | 99.99599.99699.99699.995 | 99.99899.99899.99899.998 |

Table 3: Effect of different stripped agents

|  |  |
| --- | --- |
| % Extraction | Stripping agents |
| 1.859699100 | 1 M NH33 M NH35 M NH38 M NH3 |
| 0.020.020.020.02 | 1 M HClO43 M HclO45 M HclO48 M HclO4 |
| 0.020.0750.020.02 | 1 M H2SO43 M H2SO45 M H2SO48 M H2SO4 |

|  |  |
| --- | --- |
| TOA%Extraction % | **a****b**TOA%Extraction % |
| TOA%Extraction % | **d****c**TOA%Extraction % |

Figure 1: Effect of TOA% on palladium extraction in different solvents (a: toluene, b: xylene, c: crosin and d: 1, 2 dichloroethane).

Figure 2: Variation of the palladium (Ⅱ) extraction with the HCl concentration (200 ppm Pd (Ⅱ) in 0.05-8 M; 2.5% TOA in toluen; A: O (v/v) = 1; room temperature; 10 min).

Figure 3: The effect of HClO4 concentration on stripping

Figure 4: The effect of H2SO4 concentration on stripping

Figure 5: The effect of NH3 concentration on stripping